Spring Research Project

Mentor:

Mentee:

Project Title: Quasiparticle interference mapping of Cu(111) surface

Objective: To analyze scanning tunneling microscopy (STM) images measure the effective mass of an electron on the surface of a copper crystal

Background: This project uses a few ideas from condensed matter physics that go beyond introductory undergraduate physics. You do not need to be an expert in these ideas to complete the project. The goal of this section is to give you enough background to understand what you are measuring, why the measurement is interesting, and how the analysis connects to the physics. The key concepts are introduced briefly below.

Band-structure: Electrons in a crystal behave differently from electrons in an isolated atom. In an atom, electrons occupy discrete energy levels, often labeled by quantum numbers such as n, l, and m. In a crystal, however, there is an enormous number of available states which together form energy bands. Within a band, the spacing between neighboring energy levels is so small that the electron’s energy can be approximated as continuous. In addition to discrete quantum numbers used to label the bands, a continuous quantity is used to distinguish individual states inside a band. This new quantity is called the crystal wavevector, and it is written as k. The energy, E, of electrons in a band turns out to be a function of k. We call this function, Ek, the dispersion relation. The dispersion relation contains all the useful information we need to determine how electrons behave in a crystal.

Effective mass: Surprisingly, electrons in a crystal sometimes behave similarly to free electrons, except with a different mass which we call the effective mass (m*). More accurately, the dispersion relation for electrons near the bottom of some bands takes on a parabolic form:

Ek=E0+ℏk22m*

where E0 is the energy at the bottom of the band, and ℏ=1.054×10-34 J⋅s is the reduced Planck constant. It turns out that ℏk plays a momentum-like role for electrons in a crystal, and is called the crystal momentum. If we replace ℏk with p in the above equation, then the second term becomes p22m*=12m*v2, which is just the kinetic energy of a free electron (with mass m*)!

Scanning Tunneling Microscopy: So can we actually measure Ek? In this project, you will analyze data from a scanning tunneling microscope (STM) in order to determine the dispersion relation, and the effective mass, of electrons in the sample. Before explaining the details of the data analysis, we should take a detour to explain the experimental technique, and what physical sample we are studying. For an introduction to STM, please follow this link to watch a short YouTube video: https://www.youtube.com/watch?v=HE2yE8SvHmA&ab_channel=LaPhysiqueAutrement

In summary, STM is a technique that allows us to measure both the topographic and electronic properties of surfaces with atomic-scale resolution. The operating principle is that a sharp metallic tip is positioned within 1nm of the sample, and electrons are able to quantum mechanically tunnel across the tip-sample gap due to a bias which is applied to the sample. In the interest of time, we won’t go into more detail about STM here, but more information is available online. See also: Introduction to Scanning Tunneling Microscopy by Julian Chen.

There are two main imaging modes. In constant-height mode, the tip is scanned laterally along a plane while the tunneling current is recorded. In constant-current mode, a feedback loop constantly changes the tip-sample distance while the tip is scanning in order to keep the current approximately equal to some user-specified setpoint value. In this mode, the recorded tip height yields a topographic map of the surface. All of the images (.dat) in your data set are in constant-current mode. There is also one current vs bias spectrum (.csv) included, which was taken in constant height mode.

dI/dV maps: In addition to the “topography” and “current” channels, there is a third data channel: the dI/dV signal, which is the derivative of current with respect to the bias voltage. In the image files (.dat), this channel is (confusingly) called “voltage”. In the spectrum file (.csv), this channel is called “dI/dV”. The dI/dV signal was measured using a lock-in amplifier, an instrument that can detect small changes in a signal while filtering out much of the noise. This channel is especially useful because dI/dV is approximately proportional to the local electronic density of states, which tells us where electronic states are available at a given energy. For this reason, the analysis in this project will use the dI/dV maps rather than the topography maps.

A dI/dV map is also energy-selective: it probes electronic states at an energy set by the bias voltage between the STM tip and the sample. The reference energy for this measurement is the Fermi level, which you can think of as the energy of the highest occupied electron states in the sample (at low temperature). Roughly speaking, a dI/dV map taken at sample bias V shows the local density of states at energy eV relative to the sample’s Fermi level. At zero bias, the measurement probes states at the Fermi level. At a sample bias of −1 V, it probes states about 1 eV below the Fermi level.

Scattering and standing waves: We can now move on to discuss the dI/dV maps for this particular sample. The STM data used in this project were taken on a Cu(111) surface. In this context, the notation (111) refers to a particular crystal plane within a face-centered cubic crystal (like Cu). This surface hosts a special electronic state in which electrons are effectively confined to move along the surface, forming a two-dimensional electron gas (2DEG). However, all surfaces have imperfections. There are defects, steps, and impurities (mostly CO molecules) which interrupt the translational symmetry of the surface.

When surface electrons encounter these impurities, they scatter. Because electrons have wave-like properties, the incoming and scattered electron waves can overlap and interfere with one another. This produces standing-wave patterns in the local density of states, which appear in the dI/dV maps. The wavelength of these standing waves depends on the electron energy, which is set by the sample bias. By measuring how the standing-wave wavelength changes with bias voltage, we can reconstruct the dispersion relation of the Cu(111) surface state.

For the Cu(111) surface state, the simplest and most important scattering process is “backscattering,” where an electron with wavevector +k scatters into a state with wavevector -k. The difference between the final and initial wavevectors is called the scattering wavevector:

q=Δk=kfinal-kinitial

For backscattering, q=-k-+k=-2k, so the magnitude is q=2k. The wavelength seen in the dI/dV maps corresponds to q. Therefore, if the standing-wave wavelength is λ, then q=2π/λ. Finally, if we plug q into our formula for the dispersion relation, we get:

Eq=E0+ℏq28m*
=E0+Aq2

where A=ℏ28m*. We could arrive at a value for the constant A by fitting a parabola to E vs q data. This gives us a formula for the effective mass:

m*=ℏ28A

In condensed matter physics, this process of plotting E as a function of scattering wavelength q is called “quasi-particle interference mapping”, or QPI mapping.

Data analysis: The workflow to determine effective mass is as follows

- For each dI/dV map:

  - Record the sample bias

  - Measure the scattering wavevector q

- Make a plot of E vs q

- Fit a parabola to your plot to get a value for A=ℏ28m*

- Solve for m*

A “good” answer for m*/me is anything in the range 0.38 to 0.46. However, don’t be too discouraged if your final answer is outside this range. The parabolic band approximation is not perfect far away from the band edge which is around -0.45 V  Additionally, surface contamination tends to increase the measured effective mass. A result in the range of 0.1 – 1.0 is satisfactory. In your parabolic fit, you may also get a linear and a constant term. The constant term should match the band edge -0.45 V, and the linear term we can just ignore for this project.

Gwyddion: I highly recommend that you use the Gwyddion software package (https://gwyddion.net/) to handle the .dat files. It has a handy GUI that looks like the image to the right:

Here are the main things you’ll need to do:

- To access the different data channels, click “Info  Show Data Browser”

- To find file metadata, right-click a topography image, and then click “Metadata Browswer”. Bias voltage should be one of the first entries. The constant current setpoint is called “FBLogIset”.

- To take a Fourier transform, click “Data Process  Integral Transforms  2D FFT”. Then make sure the output type is Modulus, and click OK

- To take a power spectral density function, click “Data Process  Statistics  2D PSDF”

- In the GUI, you can hover your mouse over the icons for more information. In the Tools section, two useful functions are “Extract profiles along arbitrary lines”, and “Extract angularly averaged profiles”.

A full tutorial of the Gwyddion software is beyond the scope of this document, but you should have plenty of time to play around and figure things out for yourself. Overall, learning/using Gwyddion will be a lot faster than trying to code everything in Python.

Fourier analysis: The simplest way to measure q is to measure the distance between peaks in the standing wave pattern. However, since there are waves traveling in all directions it isn’t obvious which two crests you should select to make this measurement. A much better option is to perform a 2D Fourier transform on the data. The algorithm used to perform this operation on digital signals is called the Fast Fourier Transform, or FFT. A 2D Fourier transform rewrites the image in terms of spatial frequencies. In real space, the standing waves appear as ripples around defects. In Fourier space, those ripples appear as rings. The radius of a ring tells us the dominant scattering wavevector q for that image.

Note: there is one annoying convention to be careful about. In the Gywddion image analysis software package, when you do a 2D-FFT, the Fourier axes are ordinary spatial frequencies, with units of cycles per length f=1λ. In physics, however, we usually define a wavevector using radians per length q=2πλ. Depending on the exact Gwyddion tool used, the Fourier-space axis may already include this factor of 2π. If you instead calculate the power spectrum (the magnitude squared of the FFT) then Gwyddion won’t include the 2π in the axes. To check the convention, measure the wavelength λ directly from a line profile through the standing-wave pattern in real space. Then compare the Fourier-ring radius to both 1/λ and 2π/λ. If you’re still uncertain, you can check the documentation.

You may also notice that the Fourier transform contains more than one ring. The ring of interest comes from scattering of the Cu(111) surface-state electrons, which form the two-dimensional electron gas discussed above. Another ring can appear due to scattering involving bulk electronic states. For this project, focus on the surface-state ring, since that is the one used to reconstruct the 2D surface-state dispersion and extract the effective mass. The surface-state ring should be the one whose radius changes systematically with bias in a way that follows the expected parabolic dispersion.

Goals:

- Plot STM data using either Python or other plotting software of their choice, and apply filters as necessary

- Measure wavelength of standing wave pattern using Fourier analysis

- Plot measured wavelength vs sample bias

- Extract effective mass of the surface electrons via fit of data to theory

For lingering questions, contact William Koll at will.h.koll@gmail.com

____________________________________________________________________

Example Project Calendar (modify as needed):

| Dates: | Tasks: |
| --- | --- |
| Week 1 | Reading to understand Fourier transform. Readings to understand basic condensed matter concepts (band structure, Fermi surface) |
| Week 2 | Download files Try to plot things in Python or using plotting software like Gywddion Continue readings if necessary |
| Week 3 | Confirm that data is being plotted correctly Fourier transform data Perform basic measurements such as linecut |
| Week 4 | Readings about theoretical prediction of standing wave pattern vs sample bias Implement basic image filtering techniques to improve measurements. |
| Spring Break | None |
| Week 5 | Settle on a strategy or strategies for measuring standing pattern wavelength(s). Can be done with linecuts in real image or FFT, but student should at least compare with FFT. Student can start recording wavelength vs sample bias measurements. |
| Week 6 | Finish measurements of standing wave pattern wavelength. Plot results. |
| Week 7 | Fit parabola to above results From fit, extract effective mass |
| Week 8 | Work on poster |
| Week 9 | Present poster! |

Reading List:

- Basic Fourier transform intro:

  - 3B1B video: (https://www.youtube.com/watch?v=spUNpyF58BY&ab_channel=3Blue1Brown)

- Some basic STM resources:

  - Youtube video: (https://www.youtube.com/watch?v=HE2yE8SvHmA&ab_channel=LaPhysiqueAutrement)

  - Textbook by Chen (for reference only – do NOT need to read whole thing)

- Some basic band structure resource

  - Khan academy youtube video: (https://www.youtube.com/watch?v=3npADYVtQOM&ab_channel=KhanAcademyIndia-English)

  - Max Lein lecture (https://www.youtube.com/watch?v=1ZpFq0W067o&t=706s&ab_channel=MaxLein)

  - CH2 of “Condensed Matter Essentials”

- Previous STM studies of Cu(111)

  - Crommie, M., Lutz, C. & Eigler, D. Imaging standing waves in a two-dimensional electron gas. Nature 363, 524–527 (1993). https://doi.org/10.1038/363524a0

- Review article on QPI mapping:

  - N.Avraham, J.Reiner, A.Kumar-Nayak, N.Morali, R.Batabyal, B.Yan, H.Beidenkopf, Adv. Mater.2018, 30, 1707628. https://doi.org/10.1002/adma.201707628

Resource List:

- Gupta group

- Free, open-source scanning probe microscopy plotting software like

  - Gywddion (http://gwyddion.net/)

  - SpectraFox (https://www.spectrafox.com/)

- Python + IDE of choice